1.103 CIVIL ENGINEERING MATERIALS LABORATORY (1-2-3)

CONCRETE II:  HARDENED PROPERTIES

data sheet (1 of 2)

================================================================

All dimensions in  ___mixed___	Group No.  ___A2______	Date:  04/06/04

================================================================

Measurement Device	Vertical Force	Act. Disp.	Lft Disp. Extr	Rgt Disp. Extr

Calibration. Factor	__100kN/V	10.0mm/V__	_32.03in/(V/V)	34.11in/(V/V)

DAQ Channel	____2______	_____3_____	______6____	____5______

Analog Gain	____1______  	____1______	____100____	____100____

Input Voltage	____1______	_____1_____	____4.000__	____4.000__

Gage Length	___2.0 in    	____2.0 in_

================================================================

Test Description  _B1 S2______	File Name	A2B1S2___	Front	Side

Specimen Height _8.1 in ,  _     _ ,     ___

Specimen Dia.  103.13 mm  102.24_ ,  102.67__ ,  _101.57_

Specimen Mass _3954_____(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  _B2 S2______	File Name	__A2B2S2_	Front	Side

Specimen Height _8.0 in_ ,  _________ ,  _________

Specimen Dia.  _101.77  _101.52 ,  _103.25,  _102.64 mm

Specimen Mass _3944_____(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  _B3 S2______	File Name	_A2B3S2__	Front	Side

Specimen Height _8.0 in___ ,  _________ ,  _________

Specimen Dia.  _101.61,  101.62 ,  _102.57 , _101.88 mm

Specimen Mass _3995_____(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  B4 S2_______	File Name	_A2B4S2___	Front	Side

Specimen Height _8.0 in__ ,  _________ ,  _________

Specimen Dia.  101.57__,  _101.77 ,  _102.07,  _102.32 mm

Specimen Mass _4019_____(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

1.103 CIVIL ENGINEERING MATERIALS LABORATORY (1-2-3)

CONCRETE II:  HARDENED PROPERTIES

data sheet (2 of  2)

================================================================

Test Description  _B5 S2__	File Name	_A2B5S2____	Front	Side

Specimen Height _8.1  in__ ,  _________ ,  _________

Specimen Dia.  _103.23,  102.00 ,  101.45,  _101.49 mm_

Specimen Mass _4014_____(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  ____________	File Name	__________	Front	Side

Specimen Height _________ ,  _________ ,  _________

Specimen Dia.  _______,  ______ ,  _______ ,  _______

Specimen Mass __________(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  ____________	File Name	__________	Front	Side

Specimen Height _________ ,  _________ ,  _________

Specimen Dia.  _______,  ______ ,  _______ ,  _______

Specimen Mass __________(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  ____________	File Name	__________	Front	Side

Specimen Height _________ ,  _________ ,  _________

Specimen Dia.  _______,  ______ ,  _______ ,  _______

Specimen Mass __________(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================

Test Description  ____________	File Name	__________	Front	Side

Specimen Height _________ ,  _________ ,  _________

Specimen Dia.  _______,  ______ ,  _______ ,  _______

Specimen Mass __________(gm)          Vin __________

Zero Lt-LVDT  ________  Zero Rt-LVDT __________

Zero Load   _______

================================================================